### 3885	Rolled Erosion Control Products

### 3885.1	SCOPE

Provide temporary rolled out products to control erosion, aid the establishment of vegetation, and reinforce vegetation, and temporary reinforce slopes, ditch bottoms, and shorelines.  Provide netting opening dimensions large enough to germinate plants, reduce animal entanglement, and keep fill material intact.

### 3885.2	REQUIREMENTS

A	Erosion Control Blanket Requirements

Provide blankets that conform to the general requirements listed in Table 3885-1, Table 3885-2, and Table 3885-3

| Table 3885-1 Erosion Control Blanket Criteria |  |  |  |
| --- | --- | --- | --- |
| Criteria |  | Category 0 |  |
|  |  | Wood Cellulose Fiber 1S, NT | Wood Fiber 0S |
| mass per yd2 (min) ASTM D 6475 |  | 6.0 oz | 8.0 oz |
| Permissible Shear stress, Minimum (non-vegetated) ASTM D 6460 |  | 0.5 lb/Sq. ft. | 0.5 lb/sq. ft. |
| Target Service Life |  | 3 months | 3 months |
| Fill | Fiber length, 80% greater than | 0.5 in | 6 in |
|  | Material | 100% Wood Cellulose | 100% Excelsior |
| Netting | Material | Degradable | - |
|  |  |  | - |
|  | Degradation ASTM D4329, Cycle A | <3 months | - |
| Stitching | Material | - | Degradable |
|  | Degradation ASTM D4329, Cycle A | - | <3 months |
|  | Max spacing |  | 4 in |
| 0S – No netting, stitching only 1S – Netting on one side NT – No thread/stitching |  |  |  |

| Table 3885-2 Erosion Control Blanket Criteria |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Criteria |  |  |  | *Category 3P, Category 3N |  | *Category 4P, Category 4N |  |
|  |  |  |  | Straw 2S | Wood Fiber 2S | Straw-Coconut 2S | Wood Fiber 2S |
| mass per yd2 (min) ASTM D 6475 |  |  |  | 6.0 oz | 6.0 oz | 8.0 oz | 8.0 oz |
| Permissible Shear stress, (min) (non-vegetated) ASTM D6460 |  |  |  | 1.75 lb/sq. ft | 1.75 lb/sq. ft | 2.00 lb/sq. ft | 2.00lb/sq. ft |
| Tensile Strength ASTM D6818 |  | MD |  | >75 lbs/ft |  | >100 lbs/ft |  |
|  |  | TD |  | >40 lbs/ft |  | >40 lbs/ft |  |
| Fill | Fiber length, 80% greater than |  |  | 3 in | 6 in | 3 in | 6 in |
|  | Material |  |  | 100% Straw | 100% Excelsior | 70% Straw, 30% Coconut | 100% Excelsior |
|  | Target Service Life |  |  | 12 months | 12 months | 24 months | 24 months |
| Netting | Material |  |  | **Degradable Synthetic or Natural | **Degradable Synthetic or Natural | **Degradable Synthetic or Natural | **Degradable Synthetic or Natural |
|  | Netting Degradation ASTM D4329 Cycle A |  |  | 6 months | 6 months | 9 months | 9 months |
| Stitching | Material |  |  | **Degradable Synthetic or Natural | **Degradable Synthetic or Natural | **Degradable Synthetic or Natural | **Degradable Synthetic or Natural |
|  | Stitching Degradation ASTM D4329, Cycle A |  |  | 3 months | 3 months | 3 months | 3 months |
| 2S – Netting on two sides * 3P &4P = Synthetic netting, 3N & 4N = Natural netting and natural stitching ** combination of photo, heat, and moisture degradation |  |  |  |  |  |  |  |

| Criteria | Table 3885-3 Erosion Control Blanket Criteria |  |
| --- | --- | --- |
|  | Category 6 |  |
|  | Straw-Coconut 3S | Wood Fiber 3S |
| Min mass per yd2 ASTM D 6475 | 10.2 oz | 10.2 oz |
| Fiber Length, 80% greater than | 3 in | 6 in |
| Material | 70% Straw and 30% Coconut Fibers | 100% Excelsior Fibers |
| Netting and Stitching Target Service Life | 36 months | 36 months |
| Netting and Stitching Material | Black UV Stabilized Polypropylene | Black UV Stabilized Polypropylene |

A.1	Material Fiber

Provide fill material with a uniform web of interlocking fibers, with uniform thickness, and with the material fibers evenly distributed over the entire area of the blanket.

A.2	Anchors

Provide anchors for each category of blanket meeting the requirements in Table 3885-4.

| Table 3885-4 Anchor Specification |  |  |  |
| --- | --- | --- | --- |
| Blanket Category | Material | Type | Minimum Length, in |
| 0 | Biodegradable | Stake | 5 |
| 3 and 4* | Steel Wire | 11 Gauge | 6 |
| 6 | Steel Wire | 11 Gauge | 8 |
| * For frozen ground use 60D common nail with washer |  |  |  |

B	Turf Reinforcement Mat Requirements

Provide Turf Reinforcement Mats (TRM) made of a three-dimensional matrix of synthetic material, continuously bonded at filament intersections meeting the requirements of Table 3885-5.  Fill all Turf Reinforcement Mats (TRM) with soil.

| Table 3885-5 Turf Reinforcement Mat Criteria |  |  |  |
| --- | --- | --- | --- |
| TRM Category | Minimum Permissible Shear Stress ║, lb/sq ft | Minimum Tensile Strength †, lb/ft ASTM-D 6818 | Matrix Composition ‡ |
| 1 | 2.1 | 125 | Nylon, Polypropylene, Polyolefin, or Polyester |
| *2 | 6 | 150 | Nylon, Polypropylene, Polyolefin, or Polyester |
| *3 | 8 | 175 | Nylon, Polypropylene, Polyolefin, or Polyester |
| *4 | 10 | 1370 | Nylon Polypropylene, Polyolefin, or Polyester |
| * Provide mats with cells at least ⅜ - ¾ in in depth to allow soil filling and retention. ║ ASTM D 6460-07 vegetated. † Minimum Average Roll Value of either direction. ‡ , UV stability ASTM D4355 at 500 hours of 80 percent. |  |  |  |

B.1	Fill Material

Fill category 2, 3, and 4 Turf Reinforcement Mats (TRM) with 1/2 in soil meeting table 3877-3, “sandy clay loam topsoil borrow”.

B.2	Anchors

Provide anchors for Turf reinforcement Mat meeting the requirements in Table 3885-6.

| Table 3885-6 Anchor Specification |  |  |  |
| --- | --- | --- | --- |
| Blanket Category | Material | Type | Minimum Length, in |
| TRM * | Steel Wire | 11 Gauge | 10 |
| * Adjust anchor selection to assure RECP is held in place securely. |  |  |  |

C	Flexible Concrete Geogrid Mat

Provide a flexible concrete mat consisting of concrete blocks meeting requirements of ASTM D6684 and connected together by an interlocking geogrid.  Place the mats side by side and anchor to provide one homogeneous erosion protection system.

C.1	Physical Requirements

Provide a minimum open area of 10% that allows topsoil infilling, if specified.

Minimum permissible Shear stress as per ASTM 6460 (vegetated) 20 lbs. per sq. ft.

C.2 	Interlocking Geogrid

Interlocking geogrid shall have the following physical characteristics of Table 3885-8.

Table 3885-8 Interlocking Geogrid Characteristics

| Mass/Unit Area (min) | ASTM D‐5261 | 7.0 oz/yd2 |
| --- | --- | --- |
| Aperture Size (min) | Measured | 1.6 x 1.6 inch |
| Wide Width Tensile Strength |  |  |
| Machine Direction (MD) (Min) | ASTM D‐6637 | 2,055 lb/ft |
| Transverse Direction (TD) (min) | ASTM D‐6637 | 2,055 lb/ft |
| Elongation at Break (Max) | ASTM D‐6637 | 6 % |
| Tensile Strength @ 2% |  |  |
| Machine Direction (MD) (min) | ASTM D‐6637 | 822 lb/ft |

C.3	Anchoring System

Provide Number 4 J hooked rebar, minimum 2 foot length for pneumatic driven installation depth, flush to Flexible Concrete Geogrid Mat surface.

C.4	Concrete

Provide wet cast blocks meeting Specification 2461 “Structural Concrete” and the following:

- Manufactured in a plant with a Department approved quality control plan,

- Design air content of 6.5 percent,

- Absorption no greater than 7.0 percent when tested in accordance with ASTM C 140, and

- Minimum Design Strength of 4000 psi at 28 days when tested in accordance with ASTM C 140:

D	Concrete Fabric Mat

Provide Concrete Fabric Mat (CFM) that is a cement impregnated fabric that hardens when hydrated to form a water resistant mat. It can be installed underwater and has a working time of several hours after hydration.

It shall meet the following requirements of Table 3885-9

Table 3885-9 Physical Characteristics

| Type | Thickness (in) | Dry Weight (sq ft) | Hydration Min. Water volume (gal/ft2) | Compressive strength ASTM C473-07 (10 day, psi) |
| --- | --- | --- | --- | --- |
| A | 0.20 | 1.43 | 0.2 | 5800 |
| B | 0.31 | 2.46 | 0.3 | 5800 |
| C | 0.51 | 3.89 | 0.5 | 5800 |

Provide rolls capable of handling from spreader beams or bars. Provide proper storage and handling methods capable of dry storage until placement. Provide means capable of cutting into structure configurations and openings prior to hydration and again after placement as necessary for proper fit and transport of flowing water.

D.2	Anchor Pins
Provide 3 foot long, formed crozier or U-shaped, sharpened #3 rebar pins or other manufactured recommendation anchoring systems.

D.3	Overlap and Lap-Joint Bonding Agents
Provide appropriate sealant capable of bonding to both the PVC backing and fiber surface of the Concrete Fabric Mat. The sealant must work in both wet and dry conditions prior to hydration and remain functional during hydration.

D.4	Hydration Water
Provide water to the Concrete Fabric capable of surface saturation when no longer applying water for 2 minutes. Provide sufficient water 1 hour later on fabrics thicker than 0.5 inches, ditch grades greater than 2 percent, slopes greater than 3:1, and temperatures greater than 80 degrees Fahrenheit to complete the hydration process.

### 3885.3	SAMPLING AND TESTING

Approved products for this specification are on file on the MnDOT web page in the Materials Engineering Section.

The Contractor shall inspect the flexible concrete mats upon delivery. Flexible concrete Mats missing more than 4 concrete blocks per 80 square feet section shall be rejected.