# (2331) PAVEMENT JOINT ADHESIVE

### Revised 10/17/2011

Use on longitudinal construction joints between:

1. Adjacent hot mix asphalt pavements (trafficked lanes and shoulders)

2. Hot mix asphalt pavement and adjacent concrete pavement (or curb and gutter)

Note: Not required on a longitudinal construction joint between adjacent hot mix asphalt pavements formed by echelon paving.

- DESCRIPTION

Apply the joint adhesive to the face of the longitudinal construction joint.

- MATERIAL

Provide joint adhesive meeting requirements as specified in Table 1.

TABLE 1 - JOINT ADHESIVE SPECIFICATIONS

| #### TEST | #### SPECIFICATION |
| --- | --- |
| Brookfield Viscosity, 204 °C [400 °F] ASTM D 3236 | 4,000-10,000 cp |
| Cone Penetration, 25 °C [77 °F] ASTM D 5329 | 60-100 dmm |
| Resilience, 25 °C [77 °F] ASTM D 5329 | 30% minimum |
| Ductility, 25 °C [77 °F] ASTM D 113 | 30 cm minimum |
| Ductility, 4 °C [39.2 °F] ASTM D 113 | 30 cm minimum |
| Tensile Adhesion, 25 °C [77 °F] ASTM D 5329 | 500% minimum |
| Softening Point ASTM D 36 | 77 °C [170 °F] min. |
| Asphalt Compatibility ASTM D 5329 | Pass |

- CONSTRUCTION REQUIREMENTS

A.	Equipment Requirements

Use a jacketed double boiler type melting unit, with both agitation and recirculation systems.  Provide a pressure feed wand application system.

B.	Material Handling

Submit a copy of the manufacturer's recommendations for heating, re-heating, and applying the joint adhesive material.

Do not remove the joint adhesive from the package until immediately before it is placed in the melter.  Joint adhesive boxes must be clearly marked with the name of the manufacturer, the trade name of the adhesive, the manufacturer's batch and lot number, the application/pour temperature, and the safe heating temperature.  Feed additional material into the melter at a rate equal to the rate of material used.

Verify the pouring temperature of the joint adhesive at least once per hour at the point of discharge.  Stop production if the adhesive falls below the recommended application/pour temperature.  When the temperature of the adhesive exceeds the maximum safe heating temperature, stop production, empty the melter, and dispose of that adhesive in an environmentally safe method.  No payment will be made for this material or its disposal.

Do not blend or mix different manufacturer’s brands or different types of adhesives.

C.	Joint Adhesive Application

The face of the longitudinal joint must be clean and dry before the joint adhesive is applied.  Apply the joint adhesive material to the entire face of the final lift of HMA pavement where an adjacent HMA pavement will be constructed.  The joint adhesive can also be applied to the entire face of concrete pavement where an adjacent HMA shoulder pavement will be constructed.  Recommended band thickness is approximately 3 mm [1/8”].  The use of an application shoe attached to the end of application wand is recommended.  Do not overlap the joint by greater than 12.5 mm [1/2”] at the top of the joint or 50 mm [2”] at the bottom of the joint.  Apply the joint adhesive immediately in front of the paving operation.  If the adhesive is tracked by construction vehicles, repair the damaged area and restrict traffic from driving on the adhesive.

  - QUALITY CONTROL

Acceptance of the joint adhesive material is based on the certification by the manufacturer that the sealant meets the requirements listed in Table 1.  Field sampling shall be used to verify that the delivered joint adhesive meets the requirements of the specification.  The Contractor shall take a sample from the application wand during the first 20 minutes of placing sealant from each melter on the Project in the presence of the Engineer.

Each sample shall consist of two (2) aluminum or steel sample containers with the capacity to hold 2.3 kg [5 pounds] of sealant each.  The two (2) sampling containers shall be labeled with SP number, date, time, location, manufacturer and lot number of the sealant.  Each container shall be numbered one of two, or two of two.  The Engineer reserves the right to conduct supplementary sampling and testing of the sealant material.

The Contractor shall document the locations where the material from each lot number of sealant is placed.

If a field sample fails to meet any of the requirements in Table 1, the work completed with the material from the lot that the field sample represents, shall be subject to a two percent (2%) reduction in the Contract unit price of the final lift of the plant mixed asphalt pavement.

  - METHOD OF MEASUREMENT

Measure the joint adhesive by the meter [linear foot].

- BASIS OF PAYMENT

Payment for the accepted quantity of joint adhesive at the Contract price of measure will be compensation in full for all costs of furnishing and applying the material as specified.

Item No.		Item									Unit

2331.603 	Joint Adhesive 							meter [linear foot]