# (2360) PLANT MIXED ASPHALT PAVEMENT (LOCAL AGENCY)

(2013 version (Rev. 1/4/13)) ◄DO NOT REMOVE THIS.  IT NEEDS TO STAY IN FOR THE CONTRACTORS.

□	Use on local agency projects only where the local agency does not want to evaluate longitudinal joint cores.

□	All projects will use SP2005-250 (AGG. FOR SURFACE AND BASE COURSES)

- Include SP2005-250.1 (GRADED AGGREGATE FOR BITUMINOUS MIXTURES) for all Districts but District 6 or else SP2005-250.2 (GRADED AGGREGATE FOR BITUMINOUS MIXTURES) which is only for District 6.

- Include SP2005-142.2 (PAVEMENT SURFACE SMOOTHNESS)

REVISED 1/4/13

SP2005-140.1

MnDOT 2360 is hereby deleted from the MnDOT Standard Specifications and replaced with the attached 2360 (Plant Mixed Asphalt Pavement) Specification.

## Mix Designation Numbers for the bituminous mixtures on this Project are as follows:

The Designer needs to fill in the numbers here.  Examples of what is needed are:

Type SP __ Wearing Course	SPWEB_40_

Type SP __ Non-Wearing Course	SPNWB_30_

The Designer needs to let Special Provisions know how pavement smoothness will be evaluated – by S-.2, S-.3, or S-.4.

## Pavement smoothness requirements will be evaluated by equation HMA-A or equation HMA-B or equation HMA-C as specified in 2399.3D in Section S-2399 (PAVEMENT SURFACE SMOOTHNESS) of these Special Provisions.

OR

## Pavement smoothness requirements will be evaluated by Percent Improvement as specified in Section S-2399 (PAVEMENT SURFACE SMOOTHNESS) of these Special Provisions.

OR

S-.4 will be used when pavement surface smoothness will not be evaluated on the plant mixed asphalt pavement by specification 2399.

## The sentence “In addition to the list the above pavement surface must meet requirements of 2399 (Pavement Surface Smoothness) requirements.” is deleted from 2360.3.E Surface Requirements of the attached 2360 (Plant Mixed Asphalt Pavement) Specification.  The requirements of 2360.3.E Surface Requirements will apply.

The Designer needs to include all of S-.5 to S-.13 to remove Longitudinal Joint Cores from the standard 2360 (Plant Mixed Asphalt Pavement) specification.

## The first paragraph of 2360.3.D.1 of the attached 2360 (Plant Mixed Asphalt Pavement) Specification is hereby deleted and replaced with the following:

D.1	Maximum Density

Compact the pavement to at least the minimum required maximum density values in accordance with Table 2360-19, “Required Minimum Lot Density (Mat)”.

## Table 2360-20 Longitudinal Joint Density Requirement of the attached 2360 (Plant Mixed Asphalt Pavement) Specification is hereby deleted.

## 2360.3.D.1.h Mat Density Cores of the attached 2360 (Plant Mixed Asphalt Pavement) Specification is hereby deleted and replaced with the following:

D.1.h	Mat Density Cores

Obtain four cores in each lot.  Take two cores from random locations as directed by the Engineer.  Take the third and fourth cores, the companion cores, within 1 ft [0.3 m] longitudinally from the first two cores.  Submit the companion cores to the Engineer immediately after coring and sawing.  If the random core location falls on an unsupported joint, at the time of compaction, (the edge of the mat being placed does not butt up against another mat, pavement surface, etc.) cut the core with the outer edge of the core barrel 0.3 meters [1 foot] away (laterally) from the edge of the top of the mat (joint).  If the random core location falls on a confined joint (edge of the mat being placed butts up against another mat, pavement surface, curb and gutter, or fixed face), cut with the outer edge of the core barrel 150 mm ± 12.5 mm [6 inches ± 0.5 inch] from the edge of the top of the mat (ex. center of 100 mm [4 inch] core barrel 200 mm ± 12.5 mm [8 ± 0.5 inches] from the edge of the top of the mat).  Cores will not be taken within 300 mm [1 foot] of any unsupported edge.  The Contractor is responsible for maintaining traffic, coring, patching the core holes, and sawing the cores to the paved lift thickness before density testing.

The Engineer may require additional density lots to isolate areas affected by equipment malfunction, heavy rain, or other factors affecting normal compaction operations.

## 2360.3.D.1.j Companion Core Testing of the attached 2360 (Plant Mixed Asphalt Pavement) Specification is hereby deleted and replaced with the following:

The Department will select at least one of the two companion cores per lot to test for verification.

## 2360.3.D.1.n Longitudinal Joint Density of the attached 2360 (Plant Mixed Asphalt Pavement) Specification is hereby deleted.

## 2360.3.D.1.p Shoulders of the attached 2360 (Plant Mixed Asphalt Pavement) Specification is hereby deleted.

## Table 2360-24 Payment Schedule for Longitudinal Joint Density (SP Non-Wear and SP Shoulders, 4% Void)  of the attached 2360 (Plant Mixed Asphalt Pavement) Specification is hereby deleted.

## Table 2360-25 Payment Schedule for Longitudinal Joint Density (SP Non-wear and SP Shoulders, 3% Void)  of the attached 2360 (Plant Mixed Asphalt Pavement) Specification is hereby deleted.

## 2360.3.D.1.r Pay Factor Determination of the attached 2360 (Plant Mixed Asphalt Pavement) Specification is hereby deleted.