## Slide 1: NRRA Flexible Team Subcommitee #3 Rehabilitation of SFDR Cells at MnROAD March 30, 2021

## Slide 2: Meeting objectives: Develop research/construction project that provides valuable research and a safe ride for the next 5 years. Write 2-pager Reminder: This meeting is a discussion of idea for MnROAD construction in 2022. RFPs will be developed at a later date.

## Slide 3: Cross Section & Ride
Ride collected in March and May 2019
March spikes have returned
Cell 4 IRI > 2 (m /km)
Mainly due to patched area
Cell 2 and 3 still very good ride

## Slide 4: Summary
Cell 2 & 3– cores taken in low severity fatigue area.
Surface cracks only
Cell 4 – HMA layer and EE layer separated in 3 out of 4
cores. EE layer removed in pieces in 3 out of 4 cores.
HMA layer had little cracking throughout even
in locations were EE layer was removed in
pieces. Unable to determine if EE was previously
deteriorated or damaged during coring.Likely
a combination of the two

## Slide 5: Cell 2-1
Driving lane IWP
Area classified as low severity fatigue
Cracks do not extend beyond surface

## Slide 6: Cell 2-2
Driving lane IWP
Area classified as low severity fatigue
Cracks do not extend beyond surface

## Slide 7: Cell 3-1
Driving lane IWP
Area classified as low severity fatigue
Cracks do not extend beyond surface

## Slide 8: Cell 3-2
Driving lane IWP
Area classified as low severity fatigue
Cracks do not extend beyond surface

## Slide 9: Cell 4
Able to feel rigid Flyash layer during coring/ removal of loose EE layer
but decided to leave FA layer in-place

## Slide 10: Cell 4-1
Passing lane in transition BWP
4-1
No cracking

## Slide 11: Cell 4-2
Passing lane in transition OWP
4-2
Cracks only in surface

## Slide 12: Cell 4-3
Driving lane BWP
No surface distress

## Slide 13: Cell 4-4
Driving lane OWP
surface cracking = low severity fatigue

## Slide 14: Cell 2

## Slide 15: Cell 3

## Slide 16: Cell 4
Microsurface applied in October 2020

## Slide 17: Cell 4

## Slide 18: NRRA Subcommittee #3
Recommend:
  Cells 2-3 = 1-2” mill + overlay
    Could use UTBWC or thin SMA idea
  Cell 4 needs full depth fix? How deep?
OPEN DISCUSSION / MEETING NOTES WILL GO HERE

## Slide 19: NRRA Subcommittee #3
Meeting notes:
Ben W. – Research beyond construction?
Dan Wegman – recommend microsurface on 2 and 3 since ride is still good. Micro over UTBWC will create a cape seal.
  Cell 4 – want to look at salvaging with restabilizing options
    Mill 6-8” and fix FDR + flyash
    Terry B agrees
    Ben W agrees on 2-3
      Cell 15 has full depth HMA and could be redo of Cell 4
    Joel U. likes UTBWC on 2-3.
      Is micro-mill an option?
      Cell 4 opportunity to do something deeper with materials
    Steve H – cell 2/3 is cracking only in surface or through HMA should determine mill or slurry
      Cell 4 – Can this fix be applied to network situations?

## Slide 20: Notes
Dan W. – D3 uses micro on similar type applications
John G. – agrees with UTBWC. Micromill 3/8” to ½”
Jerry – 1 microsurface; 1 micro mill + UTBWC wants microsurface on 2 or 3 with additional emulsion. Micromill and ultrathin could be huge ride improvement
Dan W – not all microsurfaces are the same. Need high quality application and materials
Jenna – likes Jerry’s idea of splitting 2/3 . Need to have micro dialed in
  Cell 4 – like using inplace materials to rehab
Ben W split individual cells
  What is research goal???
    2-3 Joel “what do we do to keep extending pavement life with limited work”
    4 how to fix?