Performance Measurements

IRI – The International Roughness Index is typically reported in units of inches/mile (vertical inches of movement per mile traveled).  If a pavement were perfectly smooth the IRI would be zero. The greater the IRI the rougher the roadway.

RQI – Ride Quality Index, often converted from IRI, on a scale of 0.0 to 5.0, representing driver opinion.  RQI is calibrated to IRI by driving people, a rating panel, over sections of pavement and getting their opinion as to how well it rides.  Also noted as Present Serviceability Rating (PSR) or Present Serviceability Index (PSI).  Typical RQI rating categories and ranges are as follows:

4.1 - 5.0 	Very Good

3.1 - 4.0 	Good

2.1 - 3.0 	Fair

1.1 - 2.0	Poor

0.0 - 1.0 	Very Poor

SR – Surface rating used to quantify the amount and severity of observable and measurable pavement distresses that include cracks, spalls, rutting, faulting, patching, etc. …   The SR uses a 0.0 to 4.0 rating scale, the higher the number the less cracking is present.  A brand new road has a SR of 4.0.  As the type,

amount and severity of the various defects increase, the SR drops.  Also referred to as Pavement Condition Rating (PCR).

PQI – A composite index providing an overall indication of the condition of the pavement, taking into account both the pavement smoothness and cracking.      PQI = RQI*(SR)

Thin Surface Treatments

Thin Overlay (with or without milling):

Standard specification dense graded HMA mixture placed “Less Than” 2 inches deep ?

Common mix types – dense graded HMA

Conventional Paving Equipment

Improves Smoothness, reduce patching, and extends pavement performance period

Thinlay (with or without milling):

An HMA mixture placed in a lift thinner than 1" deep; a separate subcategory of thin overlay.

Micro-Milling / Surface Planing / Fine Milling

Similar to the traditional/standard milling process.  Micro-Milling uses a milling head/drum with more teeth at a tighter lacing pattern resulting in a surface that is smoother than the traditional milling head/drum.  This smoother surface provides a better surface for thin overlays and surface treatments including porous lifts.

Hot in-place recycling (HIR)

An on-site, in-place method performed to correct shallow depth surface distresses such as raveling, cracks, ruts, shoves and bumps to a typical depth of 1-inch and ranging from ¾ to 2-inches.  The general process consists of the following four steps:

- Softening of the asphalt pavement surface with heat;

- Scarification and/or mechanical removal of the surface material;

- Mixing of the material with recycling agent, asphalt binder, or new mix; and

- Paving of the recycled mix on the pavement surface.

Open Graded Friction Courses (OGFC), also known as Plant Mix Seal Courses

HMA paving material primarily composed of single size coarse aggregate and a generally high asphalt content with a relatively large percentage of air voids intended to provide good friction characteristics and eliminate hydroplaning for pavement surfaces.

Texas Under Seal

A chip seal placed on existing roadways before placing an overlay.

Stress Absorbing Membrane Inter-layer (SAMI)

Ultra Thin Bonded Wearing Course / Paver Placed Surface Seal / Nova Chip:

A heavy spray application of polymer modified asphalt emulsion followed immediately by an ultra-thin gap-graded hot mix asphalt (5/8" to 3/4") as a wearing course.

The thick polymer asphalt membrane seals and protects the surface and provides superior bonding of the ultrathin mix to the pavement.  Both applications are quick completed in one pass by a specially designed paving machine.  Once the hot mixed asphalt is placed, a 10-ton steel wheeled vibratory roller is used for compaction.

Microsurfacing

Microsurfacing is a form of slurry seal that uses advanced polymer additives with the emulsified asphalt.  The polymer modified emulsion, 100 percent crushed aggregate, water, and mineral filler is pre-mixed and placed as a slurry onto a pavement.

Microsurfacing benefits from a chemically controlled curing process (rather than a thermal/drying cure process required for standard slurry seals) and the ability to stack aggregates.

Microsurfacing can be used as a pre-treatment to fill ruts and other pavement irregularities.

Slurry Seal

The application of a homogenous mixture of emulsified asphalt, water, well-graded fine aggregate and mineral filler that has a creamy fluid-like appearance when applied to an existing asphalt pavement surface.  Slurry seals are used to fill existing pavement surface defects as either a preparatory treatment for other maintenance treatments or as a wearing course. There are three basic aggregate gradations used in slurry seals:

- Type I (Fine): using 1/8" aggregate for maximum crack penetration and sealing

- Type II: using 1/4" aggregate to correct raveling, oxidation, and improve skid resistance

- Type III (coarse). using 3/8" aggregate for correcting more severe surface defects, fill slight depressions, and improve skid resistance.

Chip Seal

An application of a heavy spray application of asphalt emulsion over an existing pavement surface followed by the placement of a single layer of clean, uniform sized crushed stone that are rolled to embed the aggregate chips into the binder material.

A multiple layer chip seal (double or triple etc. …) is a built-up seal coat consisting of multiple applications of binder and aggregate.  Rolling the aggregate for embedment and sweeping should be performed between applications.  Multiple chip seals are used where a harder wearing and longer lasting surface treatment is desired.

Chip Seal Surface Treatments are commonly applied to roadways with low severity cracking, raveling, or rutting.  With a pavement in good condition a Chip Seal will provide some benefit in preventing water intrusion.

Fibermat Chip Seal

Application of a Stress Absorbing Membrane layer consisting of a rapid-setting polymer-modified asphalt emulsion, discontinuous fiberglass strands and a single size aggregate.  The goal of this layer is threefold; to provide a waterproof membrane, to delay the effects of reflective cracking with embedded with fibers, and provide a skid resistant wearing surface.

Scrub Seal

Scrub seals are a multi-stage process for application of a polymer-modified asphalt emulsion where after spray application the emulsion is pressed or scrubbed into a cracked and aged surface with a broom or squeegee.  The scrubbing forces binder into the cracks.  The resulting surface may be chipped or sanded with a layer of crushed stone or sand is applied then made smooth with a slurry or chip seal.  The final operation is several passes from a multi tired roller.

A polymer modified rejuvenating emulsion (PMRE) used as a chip binder adds flexibility, toughness, and durability by restoring the asphaltenes and maltenes balance.

Cape Seal

A Chip Seal covered by a slurry seal or microsurfacing.  Benefits include a very smooth surface with increased durability.

Fog Seal:

A typically light application of a diluted slow-setting asphalt emulsion to the surface of a pavement.  For a pavement in good condition a fog seal can slow the oxidation process or placed over a thin surface treatment such as a chip seal to enhance chip retention and performance.

Rejuvenating Fog Seal:

An application of a polymer-modified asphalt emulsion that provides a denser film thickness for increased durability and resistance to cracking.  As a rejuvenator the emulsion restores essential elements in the existing asphalt, improving its overall quality and durability.  Ideal for oxidized or raveled pavements

Bio Fog Seal:

One class of emerging products includes a Bio Fog Seal which manufacturers report provide a sustainable alternative to traditional petroleum-based products.

Otta Seal

An asphalt surface treatment constructed over an aggregate base course.  Application includes placing a graded aggregate on top of a relatively thick coating of a soft bituminous binding agent.  The binder works its way into the aggregate with rolling and traffic.  Otta seals do not add structural capacity to the roadway, the base/subbase must be designed to support the anticipated traffic loading.

Scratch Course

A leveling course of HMA constructed over an existing pavement surface to improve the rideability.  The term “scratch” relates to the screed scratching on the aggregate, as the lift

thickness is set at or just above the largest aggregate size in the mix.  The leveling scratch course is designed to fill in the low spots, ruts and cupped cracks. The leveling action is accomplished using the floating screed on the paver, with more HMA being placed in the low spots than on the high spots.

Mastic Surface or crack Treatment

A hot applied mixture of polymer modified asphalt emulsion blended with quality “fine” aggregates and catalysts.

BINDER TYPES:

- Asphalt Emulsion

- Polymer-modified emulsions (PME)

- Performance-Based Asphalt (PBA) Cements: Hot applied modified binders.

- Asphalt Rubber Binder: Binders modified with high levels of crumbed tire rubber and a high natural rubber content material

- Rejuvenating Emulsion: These are emulsions modified with rejuvenating oils (and sometimes polymers) that are used to penetrate and soften existing asphalt pavements