Compacted Concrete Cut Plan

Table 2 Experimental testing

| Evaluated performance | Cell 1 or 2 |  | Cell 3 |  | Sample size | Test method | Test description |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Lab testing of saw-cut samples |  |  |  |  |  |  |  |
|  |  | No. |  | No. | Size |  |  |
| Compressive strength (7, 28, 56 d) (N = 3) | x | 9 | x | 9 | 3 × 6″ cores | ASTM C39 | Standard test method for compressive strength of cylindrical concrete specimens |
| Flexural strength of CCP without fiber (7, 28, 56 d) (N = 3) | x | 9 |  |  | 3 × 3 × 16″ prisms | ASTM C78 | Standard test method for flexural strength of concrete (third-point loading) |
| Flexural strength of FRC (7, 28, 56 d) (N = 3) |  |  | x | 9 | 3 ×3 × 16″ prisms | ASTM C1609 | Standard test method for flexural performance of fiber-reinforced concrete (third-point loading) |
| Freeze-thaw durability (N = 3) | x | 3 | x | 3 | 3 × 4 × 16″ prism |  | Standard test method for resistance of concrete to rapid freezing and thawing, procedure A |
| Hardened air content and spacing factor (N = 2) | x | 3 | x | 3 | Part of 4” cores (4 × 1″) | ASTM C457 | Standard test method for microscopical determination of parameters of the air-void system in hardened concrete |
| 56-d permeability RCPT (N = 3) | x | 3 | x | 3 | Part of 4” cores (4 × 2″) | ASTM C1202 | Standard test method for electrical indication of concrete’s ability to resist chloride ion penetration |
| Deicer salt scaling (N = 2) | x | 2 | x | 2 | 12 × 12 × 6″ slabs Actually will be pavement depth = 6” | ASTM C 672 | Standard test method for scaling resistance of concrete surfaces exposed to deicing chemicals |
| Bulk resistivity (N = 2) | x | 2 | x | 2 | 4″ cores | ASTM C1760 | Standard test method for bulk electrical conductivity of hardened concrete |
| Drying shrinkage (after 7 d moist curing, 180 d dry curing) (N = 3) | x | 3 | x | 3 | 3×3× 11.3″ prisms | ASTM C 157 | Standard test method for length change of hardened hydraulic-cement mortar and concrete |
| Total no. of samples | 34 |  | 34 |  |  |  |  |

Assumptions:

- Cut samples 1 inch larger than sample size from Table 2

- All cut samples will be 6 inch pavement depth

- Cut sample depths for ASTM standard testing will be cut and oriented for pavement surface on top

- In determining original cut layout assumed concrete weight of 150lbs/yd3

    - Cut 5”width x 6”depth x17”length=44lbs

    - Cut 4”width x6”depth x17”length=35lbs

    - Cut 12”width x 12”length x 6”depth=80lbs

    - 6” depth = pavement depth

- All cuts should be as minimum of 6 inches from edge of pavement

- Layout plan has been developed for starting point.  Research Team will coordinate with contractor saw operator to finalize in field saw cuts-want input from contractor personnel

- Keep with the additional 15 feet additional length to ensure full compaction of samples-as the paving will taper off near the end of the additional 15 feet