Missouri University of Science and Technology

Civil, Architectural and Environmental Engineering Department

Missouri University of Science and Technology

Research Plan

Compacted Concrete Pavement

Kamal H. Khayat, PhD

August 25, 2018

1. Introduction

Due to the increasing budget constraints and decreasing time in pavement construction, there has been renewed interest in exploring the application of cost-effective and rapid pavement construction techniques. Roller-compacted concrete (RCC) is a stiff mixture of aggregate, cementitious materials, and water, that is compacted by vibratory rollers [ACI 325, 1995]. Compacted concrete pavement (CCP) is an advanced form of RCC. CCP is comprised of similar proportions as that of RCC; however, it utilizes an admixture that enables better finishing and durable surface texture. The major difference in construction is that CCP has a longer “fresh” or “green” period and requires little or no rolling that makes the riding surface more uniform and consistent. The use of CCP technology is supposed to secure smooth texture during paving.

Past research undertaken at Missouri University of Science and Technology (Missouri S&T) in collaboration with the Missouri Department of Transportation (MoDOT) for the investigating of in-situ properties of RCC mixtures demonstrated prospective application in pavement construction with acceptable performance [Khayat and Libre, 2014]. However, limited experience exists with CCP. The proposed project will investigate the performance of CCP designed with special design features and durability of surface texture that can reduce construction cost and secure safe and durable surface texture. Their fresh and hardened performance will be evaluated, and pavement quality after construction will be monitored periodically.

2. Research objectives

In order to assess the construction issues and characterize the long-term performance of the proposed CCP, three CCP test cells made with and without fiber as part of a larger project that will be constructed in Scott County, Missouri, will be designed and tested. Table 1 shows the typical characteristics of the three tested cells of CCP that will be designed with different panel sizes with and without structural synthetic macro fibers (cells 1, 2, and 3). Contractor will be paving 24 feet wide.

Table 1 Typical characteristics of the three tested cells of CCP

| Item | Cell 1 | Cell 2 | Cell 3 |
| --- | --- | --- | --- |
| Mixture | Control CCP | Control CCP | Fiber-reinforced CCP |
| Fiber content (%) | 0 | 0 | Minimum 20% (ASTM C1609) |
| Length (ft) | 500 | 500 | 250 |
| Panel size (WxLxT) | 24 ft × 15 ft × 6 in. | 24 ft × 12 ft × 6 in. | 24 ft × 15 ft × 6 in. |
| Joint size (in.) | 0.125 in. × T/4 | 0.125 in. × T/4 | 0.125 in. × T/4 |

The study aims at determining the performance of designed CCP mixtures given special design features and durability of surface texture through field implementation and detailed laboratory testing. The primary performance characteristics include mechanical properties, drying shrinkage, durability, optimum joint spacing, and enhancement of joint load transfer gained from fiber-reinforcement of the pavement.

3. Anticipated results and benefits

The results of this research project aim to add value to the current state of practice related to the use of CCP, synthesize current technical knowledge, study the potential problems associated with using CCP in pavement construction in Missouri, and propose guidelines on how to avoid critical construction issues and poor quality issues. The study will deal with practices recognized by MoDOT and the Minnesota Department of Transportation (MnDOT). The outcomes of the research will provide guidelines for the selection of proper ingredients, mixture optimization methodology, as well as suitable design features to ensure cost-effective and durable CCP.

4. Proposed research program

The various field and laboratory research tasks that will be undertaken by Missouri S&T are elaborated below. Table 2 summarizes the testing program that will be conducted in this proposed research.

4.1 Field research tasks

M1 – Construction inspection

This task will include the following activities:

  - M1-A — Assist in the installation of conduits with minimal disturbance to base sub-base and slope.

  - M1-B — Monitor of the production of compacted concrete at the plant and record mixing sequences and times.

This M1-A and M1-B subtasks will be conducted by Missouri S&T in collaboration with MoDOT.

M2 – Sampling and quality control of materials during paving

This task will include the following activities:

  - M2-A — Assist with quality control tests performed before and following the paver.

  - M2-B — Develop sample fabrication procedure and sample concrete mixtures in accordance with ASTM C1435, including samples for compressive strength, flexural strength, drying shrinkage, and durability testing.

  - M2-C — An additional 15 foot will be placed at the end of each cell that samples are to be taken.  This additional 15 foot will be used for the on-site sampling according to the “Cut Plan”.  This cut plan is developed to determine how to cut this additional segment for prisms, cores, etc. for sampling.

The M2-B task will be conducted by Missouri S&T. The specimens that sampled in the field will be transported to Missouri S&T within one day. The field test results of CCP in fresh state will be analyzed and summarize in a progress report.

M3 – Lab testing and performance analysis of field samples created during paving

This task will include the following content:

  - M3-A — Conduct laboratory tests on saw-cut and cored samples.

    - Tests include: compressive strength of cylinders and flexural strength of prisms at the ages of 7, 28, and 91 d. Other tests include the freeze-thaw durability, 56-d permeability, drying shrinkage, deicer salt scaling, and hardened air-void system.

  - M3-B — Conduct laboratory tests on samples prepared during pavement construction.

    - Tests include: compressive strength of cylinders and flexural strength of prism at the ages of 7, 28, and 91 d for cells 1 and 3.

The activities will be carried out by Missouri S&T. A summary testing report will be prepared at the end of the M3 task. The analyzed results will be reported at the next scheduled bi-annual National Road Research Alliance (NRRA) meeting.

Table 2 Experimental testing

| Evaluated performance | Cell 1 or 2 |  | Cell 3 |  | Sample size | Test method | Test description |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Construction/instrumentation |  |  |  |  |  |  |  |
| Install sensors | x |  | x |  |  |  | MoDOT/Missouri S&T/MnDOT |
| Sampling preparation |  |  |  |  |  |  |  |
| Cut samples from additional 15 foot sections (noted in M2-C | x |  | x |  |  |  | These cut samples will represent the concrete on-site under high density paver compaction. |
| Create research test samples from fresh concrete during pavement construction | x |  | x |  |  | ASTM C1435 | Standard practice for molding RCC in cylinder molds using a vibrating hammer |
| Testing during paving |  |  |  |  |  |  |  |
| Quality control (density testing) | x |  | x |  |  | ASTM C1170 | Standard test method for determining consistency and density of RCC using a vibrating table |
| Surface resistivity | x |  | x |  |  |  | Test will be carried out by MoDOT |
| Early joint deployment (Periodically) | x |  | x |  |  |  | Test will be carried out by MoDOT |
| Lab testing of saw-cut and cored samples |  |  |  |  |  |  |  |
|  |  | No. |  | No. | Size |  |  |
| Compressive strength (7, 28, 56 d) (N = 3) | x | 9 | x | 9 | 3 × 6″ Cores (if not possible: 4 x 6”) | ASTM C39 | Standard test method for compressive strength of cylindrical concrete specimens |
| Flexural strength of CCP without fiber (7, 28, 56 d) (N = 3) | x | 9 |  |  | 6 × 6 × 22″ prisms | ASTM C78 | Standard test method for flexural strength of concrete (third-point loading) |
| Flexural strength of FRC (7, 28, 56 d) (N = 3) |  |  | x | 9 | 6 × 6 × 22″ prisms | ASTM C1609 | Standard test method for flexural performance of fiber-reinforced concrete (third-point loading) |
| Freeze-thaw durability (N = 3) | x | 3 | x | 3 | 3 × 4 × 16″ prisms |  | Standard test method for resistance of concrete to rapid freezing and thawing, procedure A |
| Hardened air content and spacing factor (N = 2) | x | 3 | x | 3 | Part of 4” cores (4 × 1″) | ASTM C457 | Standard test method for microscopical determination of parameters of the air-void system in hardened concrete |
| 56-d permeability RCPT (N = 3) | x | 3 | x | 3 | Part of 4” cores (4 × 2″) | ASTM C1202 | Standard test method for electrical indication of concrete’s ability to resist chloride ion penetration |
| Deicer salt scaling (N = 2) | x | 2 | x | 2 | 11 × 10 × 3″ slabs | ASTM C 672 | Standard test method for scaling resistance of concrete surfaces exposed to deicing chemicals |
| Bulk resistivity (N = 2) | x | 2 | x | 2 | 4″ cores | ASTM C1760 | Standard test method for bulk electrical conductivity of hardened concrete |
| Drying shrinkage (after 7 d moist curing, 180 d dry curing) (N = 3) | x | 3 | x | 3 | 3×3× 11.3″ prisms | ASTM C 157 | Standard test method for length change of hardened hydraulic-cement mortar and concrete |
| Total no. of samples | 34 |  | 34 |  |  |  |  |
| Lab testing of samples prepared during pavement construction |  |  |  |  |  |  |  |
|  |  | No. |  | No. | Size |  |  |
| Compressive strength (7, 28, 56 d) (N = 3) | x | 6-9 | x | 6-9 | 6 × 12″ Cylinders | ASTM C39 | Standard test method for compressive strength of cylindrical concrete specimens |
| Flexural strength of CCP without fiber (7, 28, 56 d) (N = 3) | x | 6-9 |  |  | 6 × 6 × 22″ prisms | ASTM C78 | Standard test method for flexural strength of concrete (third-point loading) |
| Flexural strength of FRC (7, 28, 56 d) (N = 3) |  |  | x | 6-9 | 6 × 6 × 22″ prisms | ASTM C1609 | Standard test method for flexural performance of fiber-reinforced concrete (third-point loading) |
| Coefficient of thermal expansion (N = 3) | x | 3 | x | 3 | 4 × 8″ cylinders |  | Coefficient of thermal expansion of hydraulic cement concrete — MoDOT |
| Total no. of the samples | Up to 21 |  | Up to 21 |  |  |  |  |
| Field data collection |  |  |  |  |  |  |  |
| Temperature/Environmental strain/ Joint Opening (hour) | x |  | x |  |  |  | Installed instrumentation — Performed by MnDOT (remotely) |
| DAQ (multi-channel, high frequency for truck load testing) | x |  | x |  |  |  | Performed by MoDOT |
| Load testing (1, 13, and 25 months) | x |  | x |  |  |  | Quarter-bridge strain gauges — Performed by MoDOT |
| Performance Data: FWD, IRI, Faultmeter, friction, visual Distress survey (1, 13, and 25 months) | x |  | x |  |  |  | Performed by MoDOT |

M4 – Sensor installation/performance monitoring

The following work will be carried out for this sub-task:

  - M4-A — Assist with sensor installation and instrumentation, including sensors of strain due to environment, dynamic load response, and joint opening, with minimal disturbance to grade. Fully document location of embedded sensors.

  - M4-B — Collect, process, and insert environmental and load response performance data into MnROAD database.

  - M4-C — Periodic (frequency to be determined) collection of load response data.

    - Includes providing periodic traffic control and loaded vehicle to conduct controlled truck loading of slabs with embedded sensors.

  - M4-D — Monitor joint deployment (periodically).

The subtask M4-A will be done by MoDOT, Missouri S&T, and MnDOT. Subtasks M4-B, M4-C, and M4-D will be carried out by MnDOT and MoDOT. MoDOT will perform:  load testing, FWD, friction testing, ride quality (IRI), joint faulting, as well as visual distress surveys.

Data will be collected by MoDOT and MnDOT and sent to Missouri S&T for analysis. A summary of data collection efforts will be prepared by Missouri S&T in collaboration with MoDOT and MnDOT.

4.2 Lab research tasks

T1 – cell performance testing and reporting

All available collected data of the three CCP cells will be gathered by MnDOT and MoDOT and organized at different cell ages of 1, 13, and 25 months.

Shortly after each data collection period, a summary report of cell behavior and trends with simple plots and discussion will be prepared by Missouri S&T and presented at next scheduled technical advisory panel (TAP) and/or bi-annual NRRA meeting.

T2 – Analysis to determine durability of surface texture

The following work will be conducted by Missouri S&T:

  - T2-A — Analyze sample test results, sensor data, and field performance data and relate it to durability of the surface texture. For example, the greater the strength of CCP, the higher resistance of CCP surface to abrasion due to traffic load. The collected sensor data due to variation of strain, temperature, load response, can reflect the quality of pavement.

  - T2-B — Determine predicted service life of surface texture as it relates to adequate friction for higher speed roads and freeze/thaw durability.

Task will be completed as sections shows noticeable distress in the surface texture, or after 2.5 years, whichever occurs first. A task report and recommendations will be made based on the observed results.

T3 – Analysis to determine impact of joint spacing and fibers on performance of CCP

To investigate the effect of joint spacing and fibers on performance of CCP, Missouri S&T will analyze data collected from the 3 cells.  Focus will be on differences in joint load transfer and the response of panels to FWD and truck loadings.

T4 – Draft final report

A draft final report will be prepared by Missouri S&T, including the following information:

  - T4-A — Summarize analysis and findings from Missouri compacted concrete test cells constructed in 2018.

  - T4-B —Provide overall conclusions and recommendations for implementation of findings.

T5 – Final report

The final report will be prepared addressing comments provided by the TAP.

  - T5-A — Create final report and publish according to MnDOT report standards.

  - T5-B — Disseminate final report to NRRA website and members.

5. Project deliverables

5.1 Progress and final reports

Progress reports will be presented at the end of each specified task. At the end of the project, a final report will be submitted, including all findings from this project. Based on the results obtained during the research process, technical papers highlighting scientific findings will be submitted to leading journals.

5.2 Formal presentations

Interim presentations will be periodically scheduled with the NRRA TAP. The final presentation will be made at a subsequent bi-annual NRRA meeting to coincide with submittal of the draft report and draft specifications.

5.3 Project schedule

The time schedule is presented in Table 3. Final reporting is planned in the form of the deliverables presented and described in the work plan.

6. Project cost

The total cost of the project will be as follows: $75,000 for year 1, $25,000 for year 2, and $25,000 for year 3, for a total of $125,000. The project start and end dates will be Sept. 15, 2018 and Sept. 14, 2021, respectively.

Table 3 Proposed time schedule

| Task | Month |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Material procurement | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33 | 34 | 35 | 36 |
| M1 Construction inspection |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| M2 Sampling during paving |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| M3 Lab testing |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| M4 Sensor installation and data analysis |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| T1 Annual report at 1, 13, and 25 months |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| T2 Surface durability analysis |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| T3 Compile data for FR-CCP |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| T4 Draft final report |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| T5 Final report |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

References

AASHTO, T336. (2009). Standard Method of Test for Coefficient of Thermal Expansion of Hydraulic Cement Concrete,” American Association of State Highway and Transportation Officials, Washington, DC.

ACI Committee 325 (1995), ACI 325-10: Report on Roller-Compacted Concrete Pavements, p. 32.

ASTM C39 (2010), Standard Test Method for Compressive Strength of Cylindrical Concrete Specimens, American Society of Testing and Materials, West Conshohocken, PA.

ASTM C78 (2010). Standard Test Method for Flexural Strength of Concrete (Using Simple Beam with Third-Point Loading) American Society of Testing and Materials, West Conshohocken, PA.

ASTM, C157 (2004). Standard Test Method for Length Change of Hardened Hydraulic-Cement Mortar and Concrete. American Society for Testing and Materials. West Conshohocken, PA.

ASTM C666 (2008). Standard Test Method for Resistance of Concrete to Rapid Freezing and Thawing. American Society of Testing and Materials, West Conshohocken, PA.

ASTM C672 (2008). Standard Test Method for Scaling Resistance of Concrete Surfaces Exposed to Deicing Chemicals. American Society of Testing and Materials, West Conshohocken, PA.

ASTM C1202 (2010). Standard Test Method for Electrical Indication of Concrete’s Ability to Resist Chloride Ion Penetration. American Society of Testing and Materials, West Conshohocken, PA.

ASTM C 1543 (2010). Standard Test Method for Determining the Penetration of Chloride Ion into Concrete by Ponding. American Society of Testing and Materials, West Conshohocken, PA.

ASTM C1170, (2010), Standard Test Method for Determining Consistency and Density of Roller-Compacted Concrete Using a Vibrating Table, American Society of Testing and Materials, West Conshohocken, PA.

ASTM C1345, (2008), Standard Practice for Molding Roller-Compacted Concrete in Cylinder Molds Using a Vibrating Hammer, American Society of Testing and Materials, West Conshohocken, PA.

Khayat, K.H., Libre, N.A. (2014). Roller compacted concrete: field evaluation and mixture optimization. No. NUTC R363. Missouri University of Science and Technology. Center for Transportation Infrastructure and Safety.